Supplementary information

Removal of Lead and Cadmium with an optimized composite of expanded graphite/g-C3N4 /phenylenediamine

Mahboobeh Zarei 1, Majid Baghdadi 2 *, Fatemeh Yazdian 3, Naser Mehrdadi 2

1Environmental Engineering, Water and Wastewater, Kish International Campus, University of Tehran, Iran.

2Department of Environmental Engineering, graduate Faculty of environment, University of Tehran, Tehran, Iran.

3Life Science Engineering, Faculty of New Sciences and Technologies, University of Tehran, Tehran, Iran.

Figs. S1-5

Tables S1-3

Figs.

| Fig. S1. Comparison of Langmuir isotherms for Pb2+ - Cd2+. |  |
| --- | --- |
| Fig. S2. Comparison of Freundlich isotherms for Pb2+ - Cd2+ (pH=5 - absorbent dosage=2 g/l -T=23 ºC - time= 60 min). |  |
| Fig. S3. Comparison of PFO (a) model and PSO (b) for Pb2+ - Cd2+(pH=5, absorbent dosage=2 g/L,T=23º C, sample volume=100 mL). |  |
| Fig. S4. Comparison of the Intra-particle diffusion (IP) model for Pb2+ - Cd2+(pH=5, absorbent dosage=2 g/L ,T=23 ºC, sample volume=100 mL). |  |
| Fig. S5. Estimation of liquid film diffusion models for Pb2+ - Cd2+(pH=5, absorbent dosage=2 g/L ,T=23 ºC, sample volume=100 mL). |  |

Table S1. ANOVA for Quadratic model.

| Source | Sum of squares | df | Mean square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 1094.28 | 9 | 121.59 | 9.31 | 0.0038 | Significant |
| A-Expanded graphite | 361.94 | 1 | 361.94 | 27.70 | 0.0012 |  |
| B-melamine | 1.81 | 1 | 1.81 | 0.1389 | 0.7204 |  |
| C-phenylenediamine | 5.41 | 1 | 5.41 | 0.4143 | 0.5403 |  |
| AB | 15.76 | 1 | 15.76 | 1.21 | 0.3084 |  |
| AC | 54.10 | 1 | 54.10 | 4.14 | 0.0813 |  |
| BC | 0.0110 | 1 | 0.0110 | 0.0008 | 0.9776 |  |
| A² | 487.08 | 1 | 487.08 | 37.28 | 0.0005 |  |
| B² | 33.50 | 1 | 33.50 | 2.56 | 0.1534 |  |
| C² | 87.67 | 1 | 87.67 | 6.71 | 0.0359 |  |
| Residual | 91.45 | 7 | 13.06 |  |  |  |
| Lack of Fit | 27.56 | 3 | 9.19 | 0.5751 | 0.6612 | Not significant |
| Pure Error | 63.89 | 4 | 15.97 |  |  |  |
| Cor Total | 1185.73 | 16 |  |  |  |  |

Table S2. Final equation in terms of coded factors.

| Remove of heavy metal | = |
| --- | --- |
| +74.99 |  |
| +6.73 | A |
| +0.4763 | B |
| +0.8225 | C |
| -1.98 | AB |
| +3.68 | AC |
| -0.0525 | BC |
| -12.36 | A² |
| -4.42 | B² |
| -6.17 | C² |

Table S3. Final equation in terms of actual factors.

| Remove of heavy metal | = |
| --- | --- |
| +45.66000 |  |
| +1.98325 | Expanded graphite |
| +1.51450 | Melamine |
| +9.52750 | phenylenediamine |
| -0.017644 | Expanded graphite * melamine |
| +0.245167 | Expanded graphite * phenylenediamine |
| -0.007000 | melamine * phenylenediamine |
| -0.054922 | Expanded graphite² |
| -0.078622 | Melamine² |
| -6.16500 | Phenylenediamine² |